Title:

Highly Ordered Arrays of Silver Nanowires for Transparent Conducting PET Film

Highlights:

- High yield synthesis of ordered arrays of purified silver nanowires (AgNWs).

- Visible photoluminescence (PL) i.e. red emission at round 700 nm.

- The AgNWs coated PET film retains its transparency and flexibility.

- The % transmittance of the PET is 92.5% with a lower sheet resistance value ~ 20 Ω.