Supporting Information for

New styryl based organic chromophores including free amino and azomethine groups: Syntheses, photophysical, NLO and thermal properties

Anka Utama Putra, Deniz Çakmaz, Nurgül Seferoğlu, Alberto Barsella, Zeynel Seferoğlu

Additional experimental, photophysical and calculated data

Table of Contents

1. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectra of compounds 3-12	2

1.1. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectra of compound 3	2

1.2. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 4	4

1.3. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 5	6

1.4. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 6	8

1.5. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 7	10

1.6. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 8	12

1.7. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 9	14

1.8. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 10	14

1.9. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 11	18

1.10. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 12	…………………….  20

2. Calculated data ……………………………………………………………………………………… 22

2.1. Optimized geometries of compounds 8-12 ……………………………………………………... 22

2.2. The calculated photophysical properties of compounds 8-12 ……………………………….. 23

3. Photophysical Properties of Compounds 3-12	24

3.1. Relative Quantum Yield Calculation Formula	24

3.2. Photoluminescence Properties of compound 3	24

3.3. Photoluminescence Properties of compound 4	25

3.4. Photoluminescence Properties of compound 5	26

3.5. Photoluminescence Properties of compound 6	27

3.6. Photoluminescence Properties of compound 7	28

3.7. Photoluminescence Properties of compound 8	29

3.8. Photoluminescence Properties of compound 9	31

3.9. Photoluminescence Properties of compound 10	32

3.10. Photoluminescence Properties of compound 11	33

3.11. Photoluminescence Properties of compound 12	34

4. Hydroxide Interaction of Compound 8-12	35

4.1. Hydroxide Interaction of Compound 8	35

4.2. Hydroxide Interaction of Compound 9	36

4.3. Hydroxide Interaction of Compound 10	37

4.4. Hydroxide Interaction of Compound 11	38

4.5. Hydroxide Interaction of Compound 12	39

5. pH Sensor properties of Compound 8 	40

6. The Calculated NLO Data	42

# 1. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectra of compound 3-12

## 1.1. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectra of compound 3

FT-IR spectrum of compound 3 in KBr

1H-NMR spectrum of compound 3 in DMSO-d6

13C-NMR spectrum of compound 3 in DMSO-d6

HR-MS spectrum of compound 3

## 1.2. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 4

FT-IR spectrum of compound 4 in KBr

1H-NMR spectrum compound 4 in DMSO-d6

13C-NMR spectrum of compound 4 in DMSO-d6

HR-MS spectrum of compound 4

## 1.3. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 5

FT-IR spectrum of compound 5 in KBr

1H-NMR spectrum of compound 5 in DMSO-d6

13C-NMR spectrum of compound 5 in DMSO-d6

HR-MS spectrum of compound 5

## 1.4. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 6

FT-IR spectrum of compound 6 in KBr

1H-NMR spectrum of compound 6 in DMSO-d6

13C-NMR spectrum of compound 6 in DMSO-d6

HR-MS spectrum of compound 6

## 1.5. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 7

FT-IR spectrum of compound 7 in KBr

1H-NMR spectrum of compound 7 in DMSO-d6

13C-NMR spectrum of compound 7 in DMSO-d6

HR-MS spectrum of compound 7

## 1.6. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 8

FT-IR spectrum of compound 8 in KBr

1H-NMR spectrum of compound 8 in DMSO-d6

13C-NMR spectrum of compound 8 in DMSO-d6

HR-MS spectrum of compound 8

## 1.7. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 9

FT-IR spectrum of compound 9 in KBr

1H-NMR spectrum of compound 9 in DMSO-d6

13C-NMR spectrum of compound 9 in DMSO-d6

HR-MS spectrum of compound 9

## 1.8. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 10

FT-IR spectrum of compound 10 in KBr

1H-NMR spectrum of compound 10 in DMSO-d6

13C-NMR spectrum of compound 10 in DMSO-d6

HR-MS spectrum of compound 10

## 1.9. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 11

FT-IR spectrum of compound 11 in KBr

1H-NMR spectrum of compound 11 in DMSO-d6

13C-NMR spectrum of compound 11 in DMSO-d6

HR-MS spectrum of compound 11

## 1.10. FT-IR, 1H-NMR, 13C-NMR and HR-MS spectrums of compound 12

FT-IR spectrum of compound 12 in KBr

1H-NMR spectrum of compound 12 in DMSO-d6

13C-NMR spectrum of compound 12 in DMSO-d6

HR-MS spectrum of compound 12

2. Calculated data

2.1. Optimized geometries of compounds 8-12.

Figure S1. The optimized geometries of 8-12.

2.2. The calculated photophysical properties of compounds 8-12

Table S1. Photophysical properties of compounds 8-12 in various solvents with different polarity and calculated absorption spectra data.

|  |  | experimental |  |  |  |  |  |  | calculated |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Solvents | λabsmax (nm) | λemmax (nm) | Stokes (nm) |  | Stokes (cm-1) | ΦFa | ε (mM-1cm-1) | λabsmax (nm) | f | Transitions | w |
| 8 | ACN (45.6c) | 543 | 644 | 101 |  | 2893 | 0.0011 | 51.409 | 521 | 1.0973 | H→L | 98.1 |
|  | DMSO (45.1c) | 562 | 650 | 88 |  | 2434 | 0.0091 | 52.973 | 524 | 1.1264 | H→L | 98.4 |
|  | DCM (40.7c) | 546 | 636 | 90 |  | 2609 | 0.0035 | 60.169 | 520 | 1.1172 | H→L | 98.4 |
|  | THF (37.4c) | 534 | 630 | 96 |  | 2871 | 0.0062 | 58.473 | 518 | 1.1075 | H→L | 98.3 |
|  | PhMe (33.9c) | 529 | 610 | 81 |  | 2517 | 0.0116 | 58.609 | 509 | 1.1082 | H→L | 98.4 |
| 9 | ACN | 510 | 623 | 113 |  | 3565 | 0.0011 | 58.272 | 501 | 1.1728 | H→L | 98.1 |
|  | DMSO | 518 | 630 | 113 |  | 3461 | 0.0083 | 54.328 | 505 | 1.1971 | H→L | 98.3 |
|  | DCM | 515 | 612 | 97 |  | 3086 | 0.015 | 40.539 | 501 | 1.1906 | H→L | 98.2 |
|  | THF | 506 | 610 | 104 |  | 3389 | 0.0072 | 54.202 | 499 | 1.1827 | H→L | 98.1 |
|  | PhMe | 504 | 581 | 77 |  | 2624 | 0.0074 | 55.824 | 491 | 1.1862 | H→L | 98.1 |
| 10 | ACN | 495 | 622 | 127 |  | 4156 | 0.0011 | 45.692 | 504 | 1.1696 | H→L | 98.2 |
|  | DMSO | 491 | 636 | 145 |  | 4643 | 0.0073 | 46.889 | 508 | 1.1929 | H→L | 98.4 |
|  | DCM | 500 | 614 | 114 |  | 3724 | 0.009 | 33.579 | 503 | 1.1865 | H→L | 98.3 |
|  | THF | 491 | 612 | 121 |  | 4037 | 0.0077 | 41.635 | 501 | 1.1787 | H→L | 98.2 |
|  | PhMe | 487 | 581 | 94 |  | 3331 | 0.0071 | 43.771 | 493 | 1.1808 | H→L | 98.2 |
| 11 | ACN | 466 | 618 | 152 |  | 5296 | 0.0012 | 42.034 | 486 | 1.1419 | H→L | 96.8 |
|  | DMSO | 467 | 625 | 158 |  | 5446 | 0.0063 | 36.536 | 489 | 1.1618 | H→L | 97.2 |
|  | DCM | 470 | 598 | 128 |  | 4565 | 0.0096 | 28.410 | 485 | 1.1593 | H→L | 96.8 |
|  | THF | 467 | 602 | 135 |  | 4802 | 0.0104 | 39.518 | 483 | 1.1535 | H→L | 96.8 |
|  | PhMe | 464 | 563 | 99 |  | 3783 | 0.0046 | 41.570 | 476 | 1.1661 | H→L | 96.4 |
| 12 | ACN | 377 | 459 | 82 | 4783 |  | - | 52.682 | 428 | 1.1826 | H-1→L H→L | 52.4 46.0 |
|  | DMSO | 385 | 496 | 111 | 5796 |  | - | 50.485 | 430 | 1.1910 | H-1→L H→L | 51.1 47.6 |
|  | DCM | 381 | 473 | 92 | 5114 |  | - | 30.407 | 430 | 1.2153 | H-1→L H→L | 55.8 42.7 |
|  | THF | 380 | 458 | 78 | 4501 |  | - | 56.907 | 429 | 1.2175 | H-1→L H→L | 56.7 41.7 |
|  | PhMe | 384 | 578 | 194 | 8729 |  | - | 53.082 | 428 | 1.2858 | H-1→L H→L | 58.3 39.8 |

aSolvents arranged in order of decreasing ET30 values. bFluorescence quantum yield (±10%) determined relative to fluorescein in pH=9 solution (FF = 1.00) as standard. cThe values for relative polarity are courtesy from Christian Reichardt, Solvent and Solvent Effect in Organic Chemistry, Wiley-VCH, 3rd ed., 2003.

# 3. Photophysical Properties of Compounds 3-12

## 3.1. Relative Quantum Yield Calculation Formula

Relative Quantum Yields of all synthesized compound are measured using equation below by taking Fluorescein (Φ = 0.95 in pH 9) as a refence.

Φs= Φr×ArAs×IsIr×ns2nr2

Φ 	: Quantum Yield

A	: Maximum absorbance value (0.055 < A < 0.095)

I	: Maximum Fluorescence value

n	: Solvent’s refractive index

Subscript “s”	: Sample

Subscript “r”	: Reference

## 3.2. Photoluminescence Properties of compound 3

Normalized absorption (left) and fluorescence (right) spectra of compound 3 in various solvents with different polarity

Photographs of compound 3 under ambient lighting (left) and 365 nm UV lamp (right) in various solvents with different polarity

Photophysical properties of compound 3 in various solvents with different polarity

|  |  |  |  |  |  | Compound 3 |
| --- | --- | --- | --- | --- | --- | --- |
| Solvent | λabsmax (nm) | λemmax (nm) | Stokes (nm) | Stokes (cm-1) | Ф | ε (mM-1cm-1) |
| MeOH | 528 | 630 | 102 | 3074 | 0.0025 | 42.625 |
| ACN | 527 | 630 | 103 | 3125 | 0.0015 | 51.729 |
| DMSO | 543 | 644 | 101 | 2879 | 0.0086 | 49.830 |
| DCM | 531 | 617 | 86 | 2632 | 0.0145 | 36.803 |
| THF | 513 | 604 | 91 | 2961 | 0.0124 | 45.871 |
| PhMe | 512 | 584 | 72 | 2414 | 0.0074 | 41.423 |

## 3.3. Photoluminescence Properties of compound 4

Normalized absorption (left) and fluorescence (right) spectra of compound 4 in various solvents with different polarity

Photographs of compound 4 under ambient lighting (left) and 365 nm UV lamp (right) in various solvents with different polarity

Photophysical properties of compound 4 in various solvents with different polarity

|  |  |  |  |  |  |  | Compound 4 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Solvent | λabsmax (nm) | λemmax (nm) | Stokes (nm) | Stokes (cm-1) | Ф | ε (mM-1cm-1) |  |
| MeOH | 498 | 606 | 108 | 3568 | 0.0042 | 55.407 |  |
| ACN | 495 | 611 | 116 | 3819 | 0.0039 | 48.590 |  |
| DMSO | 510 | 622 | 112 | 3515 | 0.0069 | 49.627 |  |
| DCM | 502 | 589 | 87 | 2954 | 0.0125 | 30.143 |  |
| THF | 486 | 582 | 96 | 3403 | 0.0083 | 33.687 |  |
| PhMe | 488 | 558 | 70 | 2592 | 0.0042 | 41.893 |  |

## 3.4. Photoluminescence Properties of compound 5

Normalized absorption (left) and fluorescence (right) spectra of compound 5 in various solvents with different polarity

Photographs of compound 5 under ambient lighting (left) and 365 nm UV lamp (right) in various solvents with different polarity

Photophysical properties of compound 5 in various solvents with different polarity

|  |  |  |  |  |  | Compound 5 |
| --- | --- | --- | --- | --- | --- | --- |
| Solvent | λabsmax (nm) | λemmax (nm) | Stokes (nm) | Stokes (cm-1) | Ф | ε (mM-1cm-1) |
| MeOH | 476 | 609 | 133 | 4599 | 0.0036 | 39.878 |
| ACN | 473 | 611 | 134 | 4770 | 0.0032 | 35.875 |
| DMSO | 486 | 624 | 138 | 4561 | 0.0067 | 42.055 |
| DCM | 483 | 592 | 109 | 3828 | 0.0137 | 25.315 |
| THF | 457 | 583 | 126 | 4741 | 0.0066 | 31.410 |
| PhMe | 467 | 557 | 90 | 3476 | 0.0046 | 33.884 |

## 3.5. Photoluminescence Properties of compound 6

Normalized absorption (left) and fluorescence (right) spectra of compound 6 in various solvents with different polarity

Photographs of compound 6 under ambient lighting (left) and 365 nm UV lamp (right) in various solvents with different polarity

Photophysical properties of compound 6 in various solvents with different polarity

|  |  |  |  |  |  | Compound 6 |
| --- | --- | --- | --- | --- | --- | --- |
| Solvent | λabsmax (nm) | λemmax (nm) | Stokes (nm) | Stokes (cm-1) | Ф | ε (mM-1cm-1) |
| MeOH | 446 | 600 | 154 | 5786 | 0.0039 | 40.765 |
| ACN | 442 | 603 | 161 | 6052 | 0.0034 | 34.575 |
| DMSO | 463 | 614 | 151 | 5346 | 0.0046 | 42.717 |
| DCM | 448 | 580 | 132 | 5099 | 0.0055 | 27.791 |
| THF | 439 | 573 | 134 | 5359 | 0.0062 | 34.745 |
| PhMe | 440 | 546 | 106 | 4399 | 0.0041 | 30.567 |

## 3.6. Photoluminescence Properties of compound 7

Normalized absorption (left) and fluorescence (right) spectra of compound 7 in various solvents with different polarity

Photographs of compound 7 under ambient lighting (left) and 365 nm UV lamp (right) in various solvents with different polarity

Photophysical properties of compound 7 in various solvents with different polarity

|  |  |  |  |  |  | Compound 7 |
| --- | --- | --- | --- | --- | --- | --- |
| Solvent | λabsmax (nm) | λemmax (nm) | Stokes (nm) | Stokes (cm-1) | Ф | ε (mM-1cm-1) |
| MeOH | 374 | Non-FLR | - | - | - | 51.433 |
| ACN | 376 | Non-FLR | - | - | - | 43.430 |
| DMSO | 386 | Non-FLR | - | - | - | 40.423 |
| DCM | 382 | 606 | 224 | 9705 | - | 42.125 |
| THF | 379 | 434 | 55 | 3357 | - | 40.418 |
| PhMe | 382 | 577 | 195 | 8853 | - | 53.152 |

## 3.7. Photoluminescence Properties of compound 8

Normalized absorption (left) and fluorescence (right) spectra of compound 8 in various solvents with different polarity

Photographs of compound 8 under ambient lighting (left) and 365 nm UV lamp (right) in various solvents with different polarity

Photophysical properties of compound 8 in various solvents with different polarity

|  |  |  |  |  |  | Compound 8 |
| --- | --- | --- | --- | --- | --- | --- |
| Solvent | λabsmax (nm) | λemmax (nm) | Stokes (nm) | Stokes (cm-1) | Ф | ε (mM-1cm-1) |
| ACN | 543 | 644 | 101 | 2893 | 0.0011 | 51.409 |
| DMSO | 562 | 650 | 88 | 2434 | 0.0091 | 52.973 |
| DCM | 546 | 636 | 90 | 2609 | 0.0035 | 60.169 |
| THF | 534 | 630 | 96 | 2871 | 0.0062 | 58.473 |
| PhMe | 529 | 610 | 81 | 2517 | 0.0116 | 58.609 |

## 3.8. Photoluminescence Properties of compound 9

Normalized absorption (left) and fluorescence (right) spectra of compound 9 in various solvents with different polarity

Photographs of compound 9 under ambient lighting (left) and 365 nm UV lamp (right) in various solvents with different polarity

Photophysical properties of compound 9 in various solvents with different polarity

|  |  |  |  |  |  | Compound 9 |
| --- | --- | --- | --- | --- | --- | --- |
| Solvent | λabsmax (nm) | λemmax (nm) | Stokes (nm) | Stokes (cm-1) | Ф | ε (mM-1cm-1) |
| ACN | 510 | 623 | 113 | 3565 | 0.0011 | 58.272 |
| DMSO | 518 | 630 | 113 | 3461 | 0.0083 | 54.328 |
| DCM | 515 | 612 | 97 | 3086 | 0.015 | 40.539 |
| THF | 506 | 610 | 104 | 3389 | 0.0072 | 54.202 |
| PhMe | 504 | 581 | 77 | 2624 | 0.0074 | 55.824 |

## 3.9. Photoluminescence Properties of compound 10

Normalized absorption (left) and fluorescence (right) spectra of compound 10 in various solvents with different polarity

Photographs of compound 10 under ambient lighting (left) and 365 nm UV lamp (right) in various solvents with different polarity

Photophysical properties of compound 10 in various solvents with different polarity

|  |  |  |  |  |  | Compound 10 |
| --- | --- | --- | --- | --- | --- | --- |
| Solvent | λabsmax (nm) | λemmax (nm) | Stokes (nm) | Stokes (cm-1) | Ф | ε (mM-1cm-1) |
| ACN | 495 | 622 | 127 | 4156 | 0.0011 | 45.692 |
| DMSO | 491 | 636 | 145 | 4643 | 0.0073 | 46.889 |
| DCM | 500 | 614 | 114 | 3724 | 0.009 | 33.579 |
| THF | 491 | 612 | 121 | 4037 | 0.0077 | 41.635 |
| PhMe | 487 | 581 | 94 | 3331 | 0.0071 | 43.771 |

## 3.10. Photoluminescence Properties of compound 11

Normalized absorption (left) and fluorescence (right) spectra of compound 11 in various solvents with different polarity

Photographs of compound 11 under ambient lighting (left) and 365 nm UV lamp (right) in various solvents with different polarity

Photophysical properties of compound 11 in various solvents with different polarity

|  |  |  |  |  |  | Compound 11 |
| --- | --- | --- | --- | --- | --- | --- |
| Solvent | λabsmax (nm) | λemmax (nm) | Stokes (nm) | Stokes (cm-1) | Ф | ε (mM-1cm-1) |
| ACN | 466 | 618 | 152 | 5296 | 0.0012 | 42.034 |
| DMSO | 467 | 625 | 158 | 5446 | 0.0063 | 36.536 |
| DCM | 470 | 598 | 128 | 4565 | 0.0096 | 28.410 |
| THF | 467 | 602 | 135 | 4802 | 0.0104 | 39.518 |
| PhMe | 464 | 563 | 99 | 3783 | 0.0046 | 41.570 |

## 3.11. Photoluminescence Properties of compound 12

Normalized absorption (left) and fluorescence (right) spectra of compound 12 in various solvents with different polarity

Photographs of compound 12 under ambient lighting (left) and 365 nm UV lamp (right) in various solvents with different polarity

Photophysical properties of compound 12 in various solvents with different polarity

|  |  |  |  |  |  | Compound 12 |
| --- | --- | --- | --- | --- | --- | --- |
| Solvent | λabsmax (nm) | λemmax (nm) | Stokes (nm) | Stokes (cm-1) | Ф | ε (mM-1cm-1) |
| ACN | 377 | 459 | 82 | 4783 | - | 52.682 |
| DMSO | 385 | 496 | 111 | 5796 | - | 50.485 |
| DCM | 381 | 473 | 92 | 5114 | - | 30.407 |
| THF | 380 | 458 | 78 | 4501 | - | 56.907 |
| PhMe | 384 | 578 | 194 | 8729 | - | 53.082 |

# 4. Hydroxide Interaction of Compound 8-12

## 4.1. Hydroxide Interaction of Compound 8

UV-Vis absorption (left) and Fluorescence (right) spectrum of compound 8 in DMSO while being treated with 40 equiv of Tetrabutylammonium hydroxide (TBAOH) and 20 equiv of Trifluoroacetic acid (TFA).

Photographs of compound 8 in DMSO under ambient lightning (left) and 365 nm UV lamp (right) while being treated with 40 equiv of Tetrabutylammonium hydroxide (TBAOH) and 20 equiv of Trifluoroacetic acid (TBAOH).

## 4.2. Hydroxide Interaction of compound 9

UV-Vis absorption (left) and Fluorescence (right) spectrum of compound 10 in DMSO while being treated with 25 equiv of Tetrabutylammonium hydroxide (TBAOH) and 10 equiv of Trifluoroacetic acid (TFA).

Photographs of compound 10 in DMSO under ambient lightning (left) and 365 nm UV lamp (right) while being treated with 25 equiv of Tetrabutylammonium hydroxide (TBAOH) and 10 equiv of Trifluoroacetic acid (TFA).

## 4.3. Hydroxide Interaction of Compound 10

UV-Vis absorption (left) and Fluorescence (right) spectrum of compound 9 in DMSO while being treated with 25 equiv of Tetrabutylammonium hydroxide (TBAOH) and 10 equiv of Trifluoroacetic acid (TFA).

Photographs of compound 9 in DMSO under ambient lightning (left) and 365 nm UV lamp (right) while being treated with 25 equiv of Tetrabutylammonium hydroxide (TBAOH) and 10 equiv of Trifluoroacetic acid (TFA).

## 4.4. Hydroxide Interaction of Compound 11

UV-Vis absorption (left) and Fluorescence (right) spectrum of compound 11 in DMSO while being treated with 25 equiv of Tetrabutylammonium hydroxide (TBAOH) and 10 equiv of Trifluoroacetic acid (TFA).

Photographs of compound 11 in DMSO under ambient lightning (left) and 365 nm UV lamp (right) while being treated with 25 equiv of Tetrabutylammonium hydroxide (TBAOH) and 10 equiv of Trifluoroacetic acid (TFA).

## 4.5. Hydroxide Interaction of Compound 12

UV-Vis absorption (left) and Fluorescence (right) spectrum of compound 12 in DMSO while being treated with 15 equiv of Tetrabutylammonium hydroxide (TBAOH) and 5 equiv of Trifluoroacetic acid (TFA).

Photographs of compound 12 in DMSO under ambient lightning (left) and 365 nm UV lamp (right) while being treated with 15 equiv of Tetrabutylammonium hydroxide (TBAOH) and 5 equiv of Trifluoroacetic acid (TFA).

# 5. pH Sensor properties of Compound 8

The calibration graph of compound 8 in water.

UV-Vis absorption (left) and Fluorescence (right) spectrum of compound 8 in Britton-Robinson buffers with different pH values

Photographs of compound 8 in Britton-Robinson buffers with different pH values

Sigmoid function obtained from compound 8 absorption spectra during pH investigation

# 6. The Calculated NLO Data

Table S2. For 8-12, the electric dipole moment (µ), the polarizability (α) and the first hyperpolarizability (βtot) and their components calculated at the B3LYP/6-31+g(d) level in gas phase. The components are in a.u.

|  | 8 | 9 | 10 | 11 | 12 |
| --- | --- | --- | --- | --- | --- |
| µx | -2.6205659 | 2.7279726 | 2.8959998 | 1.6504698 | 0.9837855 |
| µy | -4.8095355 | -4.640875 | -4.4897814 | -3.9038428 | -4.1173681 |
| µz | 0.7613633 | -0.7179775 | -0.8006226 | -0.6168524 | -1.0025078 |
| µ (D) | 14.06 | 13.81 | 13.73 | 10.89 | 11.06 |
| αxx | 748.5574454 | 732.8128266 | 758.5971407 | 726.3448376 | 736.8018793 |
| αxy | 47.483858 | -44.5969346 | -41.5528741 | -23.106799 | -26.8060878 |
| αyy | 561.4799302 | 526.4742783 | 533.1977436 | 520.0277634 | 522.927037 |
| αxz | 13.1006246 | 13.4414218 | 11.9797682 | 10.4090318 | 19.2071485 |
| αyz | -2.2817981 | 0.9751407 | 3.2955255 | 3.0487103 | 10.3803144 |
| αzz | 276.7808112 | 263.8496491 | 273.6590493 | 269.5097136 | 260.0497242 |
| α (x10-24) esu | 78.4 | 75.2 | 77.3 | 74.9 | 75.1 |
| βxxx | 7777.110412 | -8364.39289 | -10385.7216 | -8812.51513 | -2370.9643 |
| βxxy | 8910.983006 | 8898.041072 | 9347.904786 | 8792.538058 | 6171.689911 |
| βxyy | 4549.564337 | -3676.31782 | -3224.25253 | -2714.11206 | -1076.18579 |
| βyyy | 2144.20531 | 1588.065492 | 1309.96492 | 1367.639038 | 937.4977569 |
| βxxz | 343.4072648 | -436.192156 | -234.859863 | -462.2533 | -437.229565 |
| βxyz | -110.095062 | -115.78273 | -150.999268 | -140.857842 | -182.619446 |
| βyyz | 157.5326719 | -145.768547 | -176.41358 | -179.922957 | -118.306784 |
| βxzz | 36.0214645 | -31.2371137 | -47.3869433 | 46.155482 | -56.1283255 |
| βyzz | -163.82871 | -165.541833 | -153.582221 | -206.040315 | -155.785716 |
| βzzz | 149.1562889 | -141.611864 | -151.361961 | -214.391905 | -157.891706 |
| βtot(x10-30) esu | 142.5 | 137.4 | 148.9 | 131.5 | 67.5 |