Supporting information

Deterministic Model of Observed Colours on

Metal-Anodic Aluminium Oxide-Al Nanostructures

Cristina V. Manzano1,*, Jakob J. Schwiedrzik1, Gerhard Bürki1, Laszlo Pethö1,

Johann Michler1, Laetitia Philippe1

1 Empa, Swiss Federal Laboratories for Materials Science and Technology, Laboratory for Mechanics of Materials and Nanostructures, Feuerwerkerstrasse 39, CH-3602 Thun, Switzerland

Figure S1. FE-SEM micrographs of AAO films anodized in 0.3 M oxalic acid under 40 V at 3 °C with different porosity using different chemical etching times: (a) 2 min, (b) 4 min, (c) 6 min, and (d) 8 min. (e) UV-Vis reflectance spectra for AAO-Al films with different porosities before (continuous lines) and after (dotted lines) 25 nm Au sputtered on AAO-Al films. (f) Colour diagram of 25 nm Au-AAO-Al films with different porosities.

Equations for transforming Cartesian coordinates (x,y) to polar coordinates (r, θ):

r=x-xm2+y-ym2

(S1)

θ=arctany-ymx-xm

where arctan is:

arctan (y,x)=arctanyx if x>0arctanyx+π if x<0 and y≥0arctanyx-π if x<0 and y<0π2if x=0 and y>0-π2if x=0 and y<0undefined if x=0 and y=0 			         	             (S2)

The equations obtained for 10 nm Au/AAO/Al nanostructures are:

xAu,209-332nm (θ)= R(θ)·cosθ + 0.3483

y Au,209-332nm  (θ)= R(θ)·sinθ + 0.4145 	   							(S3)

where θ Au,209-332nm  (d)= -(0.35±0.04)·10-1 ·d + (9.14±1.20) with R2=0.92

and R(θ)=-(0.27±0.58)·10-2 · θ +(0.11±0.01)  for 209<d<332 nm

and

x Au,333-380nm  = R(θ)·cosθ + 0.3140

y Au,333-380nm = R(θ)·sinθ + 0.4872        								(S4)

where θ Au,333-380nm (d)= (0.66±0.25)·10-1 ·d – (23.76±8.80) with R2=0.77

and R(θ)=(9.31±0.90)·10-2·θ +(0.29±0.17)·10-1   for 333<d<380 nm

Figure S2. Thickness as a function of second anodization time for AAO films anodized in an aqueous solution of 0.3M oxalic under 40 V at 3 °C.

Figure S3. Effective refractive index as a function of the thickness for AAO films anodized in an aqueous solution of 0.3M oxalic under 40 V at 3 °C.

The equations for 8 nm Cr/AAO/Al nanostructures can now be written as a function of the effective refractive index and second anodization time, θ as function of effective refractive index (neff) is:

θCr,209-332nm (neff)= -0.36·10-1 ·(-183.84 ±52.50)∙lnneff-(1.64±0.19)4.12±1.07 + 8.75 for 209<d<332 nm

and 								                                                (S5)

θ Cr333-380nm (neff)= -0.74·10-1 ·(-183.84 ±52.50)∙lnneff-(1.64±0.19)4.12±1.07 + 27.71 for 333<d<380 nm

and θ as function of second anodization time (t2nd) is:

θCr,209-332nm (t2nd)= -0.36·10-1 ·54.23±1.43∙t2nd+(90.03±9.31)+ 8.75 for 209<d<332 nm

and  										                        (S6)

θCr,333-380nm (t2nd)= -0.74·10-1 ·54.23±1.43∙t2nd+(90.03±9.31) +27.71 for 333<d<380 nm

The equations for 10 nm Au/AAO/Al nanostructures can be written as a function of the effective refractive index and second anodization time, θ as function of effective refractive index (neff) is:

θ Au,209-332nm (neff) =-0.35·10-1·(-183.84 ±52.50)∙lnneff-(1.64±0.19)4.12±1.07 + 9.14 for 209<d<332 nm

and   											            (S7)

θ Au,333-380nm (neff)= 0.66·10-1 ·(-183.84 ±52.50)∙lnneff-(1.64±0.19)4.12±1.07- 23.76 for 333<d<380 nm

and θ as function of second anodization time (t2nd) is:

θ Au,209-332nm (t2nd) = =-0.35·10-1·54.23±1.43∙t2nd+(90.03±9.31)+ 9.14 for 209<d<332 nm

and 										                        (S8)

θ Au,209-332nm (t2nd)= 0.66·10-1 ·54.23±1.43∙t2nd+(90.03±9.31)- 23.76 for 333<d<380 nm

Figure S4. FE-SEM micrographs of AAO films: (a) cross-section of an AAO film after FIB cutting, (b)-(d) cross-section of an AAO film after FIB cutting in different parts of the sample.

Table S1. AAO thickness, x and y values obtained from the wavelength of the maximum reflectance, x and y values calculated from the reflectance and x and y calculated from the proposed model for 8 nm Cr/AAO/Al and 10 nm Au/AAO/Al nanostructures.

| 8 nm Cr/AAO/Al nanostructures |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Thickness (nm) | λmax(nm) | xλmax | yλmax | xReflctance | yReflctance | xmodel | ymodel |
| 209 ± 12 | 569 | 0.4788 | 0.5212 | 0.4115 | 0.4283 | 0.4086 | 0.4680 |
| 214 ± 10 | 671 | 0.6833 | 0.2608 | 0.5124 | 0.4170 | 0.4355 | 0.4580 |
| 251 ± 10 | 708 | 0.3958 | 0.1122 | 0.5155 | 0.3831 | 0.5230 | 0.2808 |
| 269 ± 10 | 700 | 0.7500 | 0.2500 | 0.4554 | 0.3175 | 0.4714 | 0.1930 |
| 281 ± 7 | 420 | 0.1765 | 0.0197 | 0.2572 | 0.1921 | 0.3601 | 0.1538 |
| 315 ± 5 | 450 | 0.1523 | 0.0367 | 0.2058 | 0.2065 | 0.2373 | 0.2192 |
| 318 ± 7 | 460 | 0.1402 | 0.0594 | 0.2037 | 0.2511 | 0.2279 | 0.2336 |
| 333 ± 10 | 530 | 0.2076 | 0.7661 | 0.3460 | 0.4745 | 0.3365 | 0.4782 |
| 349 ± 15 | 509 | 0.0499 | 0.8029 | 0.3350 | 0.4682 | 0.3432 | 0.4631 |
| 380 ± 15 | 540 | 0.2793 | 0.7111 | 0.3698 | 0.4833 | 0.3642 | 0.4778 |
| 10 nm Au/AAO/Al nanostructures |  |  |  |  |  |  |  |
| Thickness (nm) | λmax(nm) | xλmax | yλmax | xReflctance | yReflctance | xmodel | ymodel |
| 209 ± 12 | 536 | 0.2789 | 0.7115 | 0.3886 | 0.4326 | 0.3877 | 0.4653 |
| 214 ± 10 | 645 | 0.7056 | 0.2944 | 0.4994 | 0.4590 | 0.4086 | 0.4682 |
| 251 ± 10 | 667 | 0.6381 | 0.2399 | 0.5100 | 0.4387 | 0.5284 | 0.3860 |
| 269 ± 10 | 681 | 0.7059 | 0.2941 | 0.5003 | 0.4078 | 0.5287 | 0.3113 |
| 281 ± 7 | 748 | 0.7500 | 0.2500 | 0.4254 | 0.2792 | 0.4741 | 0.2441 |
| 315 ± 5 | 458 | 0.1392 | 0.0591 | 0.3633 | 0.2392 | 0.3723 | 0.2360 |
| 318 ± 7 | 483 | 0.1149 | 0.1092 | 0.3334 | 0.2460 | 0.3607 | 0.2410 |
| 332 ± 7 | 509 | 0.1392 | 0.0591 | 0.2955 | 0.2932 | 0.3164 | 0.2792 |
| 333 ± 10 | 511 | 0.0723 | 0.2289 | 0.2995 | 0.4720 | 0.2870 | 0.4645 |
| 349 ± 15 | 507 | 0.0056 | 0.6751 | 0.3126 | 0.4808 | 0.3048 | 0.4564 |
| 380 ± 15 | 523 | 0.1259 | 0.8094 | 0.3299 | 0.5088 | 0.3145 | 0.4873 |

Figure S5. (a) x and y calculated from the proposed model as function of x and y obtained from the reflectance. (b) x and y calculated from the wavelength of the maximum reflectance as function of x and y obtained from the reflectance.