[Electronic supporting information]

Influence of water contamination on the sputtering of silicon with low energy argon ions investigated by Molecular Dynamics simulations.

Grégoire R.N. Defoort-Levkov*1,2, Alan Bahm 3, Patrick Philipp *1

1 – Advanced Instrumentation for Nano-Analytics (AINA), Materials Research and Technology Department (MRT), Luxembourg Institute of Science and Technology (LIST), 4422 Belvaux, Luxembourg.

2 – University of Luxembourg, 4365 Esch-sur-Alzette, Luxembourg.

3 – Thermo Fisher Scientific, Hillsboro, OR, 97124, USA

Email: Patrick Philipp – Patrick.philipp@list.lu

* Corresponding author

The manuscript was written through contributions of all authors. All authors have given approval to the final version of the manuscript.

Index

DFT data fitting plots
Graph 1. Plot of the Ar – Si details with fitting parameters D0, α and r0 used in the LAMMPS script to output the potential. The full potential is displayed
Graph 2. Plot of the Ar – Si details with fitting parameters D0, α and r0 used in the LAMMPS script to output the potential. A focused part is displayed, putting accent on the potential well describing the inter-atomic forces (switch from repulsive to attractive part of the potential).
Graph 3. Plot of the Ar – O details with fitting parameters D0, α and r0 used in the LAMMPS script to output the potential. The full potential is displayed
Graph 4. Plot of the Ar – O details with fitting parameters D0, α and r0 used in the LAMMPS script to output the potential. A focused part is displayed, putting accent on the potential well describing the inter-atomic forces (switch from repulsive to attractive part of the potential).
Graph 5. Plot of the Ar – H details with fitting parameters D0, α and r0 used in the LAMMPS script to output the potential. The full potential is displayed
Graph 6. Plot of the Ar – H details with fitting parameters D0, α and r0 used in the LAMMPS script to output the potential. A focused part is displayed, putting accent on the potential well describing the inter-atomic forces (switch from repulsive to attractive part of the potential).
Graph 7. Plot of the Ar – Ar details with fitting parameters D0, α and r0 used in the LAMMPS script to output the potential. The full potential is displayed
Graph 8. Plot of the Ar – Ar details with fitting parameters D0, α and r0 used in the LAMMPS script to output the potential. A focused part is displayed, putting accent on the potential well describing the inter-atomic forces (switch from repulsive to attractive part of the potential)

G(r) per slab and grouping details
Graph 9..Plot of the detailed radial distribution functions for each slabs, with a color grading depending of the region for 100 ev, 0° bombardements, after 500 simulations

Graph 10..Plot of the detailed radial distribution functions for each slabs, with a color grading depending of the region for 100 ev, 45° bombardements, after 500 simulations

Graph 11..Plot of the detailed radial distribution functions for each slabs, with a color grading depending of the region for 100 ev, 75° bombardements, after 500 simulations

ReaxFF Potential

Table 1. Force field parameters, from “Oxidation of Silicon Carbide by O2 and H2O: A ReaxFF Reactive Molecular Dynamics Study, Part I” by David A. Newsome. et. al. - J. Phys. Chem. C 2012, 116, 30, 16111–16121.

Graph 1. Ar – Si Potential, full potential

Graph 2. Ar – Si Potential, focused part of the potential

Graph 3. Ar – O Potential, full potential.

Graph 4. Ar – O Potential, focused part of the potential

Graph 5. Ar – H Potential, full potential.

Graph 6. Ar – H Potential, focused part of the potential

Graph 7. Ar – Ar Potential, full potential

Graph 8. Ar – Ar Potential, focused part of the potential

G(r) per slab and grouping details

Graph 9 Detailed g(r) for each slab for 100 ev, 0° and 500 bombardments

Graph 10 Detailed g(r) for each slab for 100 ev, 45° and 500 bombardments

Graph 11 Detailed g(r) for each slab for 100 ev, 75° and 500 bombardments

ReaxFF potential 	
Table 1. Details of the ReaxFF potential used in the simulations.

Reactive MD-force field: c/h/o/Si/C August 3
39 ! Number of general parameters 
50.0000 !Overcoordination parameter 
9.5469 !Overcoordination parameter 
26.5405 !Valency angle conjugation parameter 
1.5105 !Triple bond stabilisation parameter 
6.6630 !Triple bond stabilisation parameter 
0.0000 !C2-correction 
1.0588 !Undercoordination parameter 
4.6000 !Triple bond stabilisation parameter 
12.1176 !Undercoordination parameter 
13.3056 !Undercoordination parameter 
-70.1292 !Triple bond stabilization energy 
0.0000 !Lower Taper-radius 
10.0000 !Upper Taper-radius 
2.8793 !Not used 
33.8667 !Valency undercoordination 
6.0891 !Valency angle/lone pair parameter 
1.0563 !Valency angle 
2.0384 !Valency angle parameter 
6.1431 !Not used 
6.9290 !Double bond/angle parameter 
0.3989 !Double bond/angle parameter: overcoord 
3.9954 !Double bond/angle parameter: overcoord 
-2.4837 !Not used 
5.7796 !Torsion/BO parameter 
10.0000 !Torsion overcoordination 
1.9487 !Torsion overcoordination 
-1.2327 !Conjugation 0 (not used) 
2.1645 !Conjugation 
1.5591 !vdWaals shielding 
0.1000 !Cutoff for bond order (*100) 
2.1365 !Valency angle conjugation parameter 
0.6991 !Overcoordination parameter 
50.0000 !Overcoordination parameter 
1.8512 !Valency/lone pair parameter 
0.5000 !Not used 
20.0000 !Not used 
5.0000 !Molecular energy (not used) 
0.0000 !Molecular energy (not used) 
2.6962 !Valency angle conjugation parameter 
7 ! Nr of atoms; cov.r; valency;a.m;Rvdw;Evdw;gammaEEM;cov.r2;# 
alfa;gammavdW;valency;Eunder;Eover;chiEEM;etaEEM;n.u. 
cov r3;Elp;Heat inc.;n.u.;n.u.;n.u.;n.u. 
ov/un;val1;n.u.;val3,vval4 
C 1.3825 4.0000 12.0000 1.9133 0.1853 0.9000 1.1359 4.0000 
9.7602 2.1346 4.0000 33.2433 79.5548 5.8678 7.0000 0.0000 
1.2104 0.0000 199.0303 8.6991 34.7289 13.3894 0.8563 0.0000 
-2.8983 2.5000 1.0564 4.0000 2.9663 0.0000 0.0000 0.0000 
H 0.7853 1.0000 1.0080 1.5904 0.0419 1.0206 -0.1000 1.0000 
9.3557 5.0518 1.0000 0.0000 121.1250 5.3200 7.4366 1.0000 
-0.1000 0.0000 62.4879 1.9771 3.3517 0.7571 1.0698 0.0000 
-15.7683 2.1488 1.0338 1.0000 2.8793 0.0000 0.0000 0.0000 
O 1.2477 2.0000 15.9990 1.9236 0.0904 1.0503 1.0863 6.0000 
10.2127 7.7719 4.0000 36.9573 116.0768 8.5000 8.9989 2.0000 
0.9088 1.0003 60.8726 20.4140 3.3754 0.2702 0.9745 0.0000 
-3.6141 2.7025 1.0493 4.0000 2.9225 0.0000 0.0000 0.0000 
N 1.2333 3.0000 14.0000 1.9324 0.1376 0.8596 1.1748 5.0000 
10.0667 7.8431 4.0000 32.2482 100.0000 6.8418 6.3404 2.0000 
1.0433 13.7673 119.9837 2.1961 3.0696 2.7683 0.9745 0.0000

-4.3875 2.6192 1.0183 4.0000 2.8793 0.0000 0.0000 0.0000 
S 1.9401 2.0000 32.0600 2.0629 0.2095 1.0316 1.5483 6.0000 
9.9553 4.9055 4.0000 52.9998 112.1416 6.5181 8.2345 2.0000 
1.4601 9.6977 71.1843 5.7487 23.2859 12.7147 0.9745 0.0000 
-11.0200 2.7266 1.0338 6.2998 2.8793 0.0000 0.0000 0.0000 
Si 2.0291 4.0000 28.0600 2.0043 0.1247 0.8218 1.5023 4.0000 
13.0000 2.0618 4.0000 11.8211 136.4845 1.8038 7.3852 0.0000 
-1.0000 0.0000 126.5182 3.6038 8.5961 0.2368 0.8563 0.0000 
-3.5163 4.2105 1.0338 6.2998 2.5791 0.0000 0.0000 0.0000 
X -0.1000 2.0000 1.0080 2.0000 0.0000 1.0000 -0.1000 6.0000 
10.0000 2.5000 4.0000 0.0000 0.0000 8.5000 15.0000 0.0000 
-0.1000 0.0000 127.6226 8.7410 13.3640 0.6690 0.9745 0.0000 
-11.0000 2.7466 1.0338 6.2998 2.8793 0.0000 0.0000 0.0000 
19 ! Nr of bonds; Edis1;LPpen;n.u.;pbe1;pbo5;13corr;pbo6 
pbe2;pbo3;pbo4;n.u.;pbo1;pbo2;ovcorr 
1 1 156.5953 100.0397 80.0000 -0.8157 -0.4591 1.0000 37.7369 0.4235 
0.4527 -0.1000 9.2605 1.0000 -0.0750 6.8316 1.0000 0.0000 
1 2 170.2316 0.0000 0.0000 -0.5931 0.0000 1.0000 6.0000 0.7140 
5.2267 1.0000 0.0000 1.0000 -0.0500 6.8315 0.0000 0.0000 
2 2 156.0973 0.0000 0.0000 -0.1377 0.0000 1.0000 6.0000 0.8240 
2.9907 1.0000 0.0000 1.0000 -0.0593 4.8358 0.0000 0.0000 
1 3 160.4802 105.1693 23.3059 -0.3873 -0.1613 1.0000 10.8851 1.0000 
0.5341 -0.3174 7.0303 1.0000 -0.1463 5.2913 0.0000 0.0000 
3 3 60.1463 176.6202 51.1430 -0.2802 -0.1244 1.0000 29.6439 0.9114 
0.2441 -0.1239 7.6487 1.0000 -0.1302 6.2919 1.0000 0.0000 
1 4 134.1215 140.2179 79.9745 0.0163 -0.1428 1.0000 27.0617 0.2000 
0.1387 -0.3681 7.1611 1.0000 -0.1000 5.0825 1.0000 0.0000 
3 4 130.8596 169.4551 40.0000 0.3837 -0.1639 1.0000 35.0000 0.2000 
1.0000 -0.3579 7.0004 1.0000 -0.1193 6.8773 1.0000 0.0000 
4 4 157.9384 82.5526 152.5336 0.4010 -0.1034 1.0000 12.4261 0.5828 
0.1578 -0.1509 11.9186 1.0000 -0.0861 5.4271 1.0000 0.0000 
2 3 180.4373 0.0000 0.0000 -0.8074 0.0000 1.0000 6.0000 0.5514 
1.2490 1.0000 0.0000 1.0000 -0.0657 5.0451 0.0000 0.0000 
2 4 231.8173 0.0000 0.0000 -0.3364 0.0000 1.0000 6.0000 0.4402 
8.8910 1.0000 0.0000 1.0000 -0.0327 6.5754 0.0000 0.0000 
1 5 129.1942 74.3656 55.2528 0.1066 -0.5211 1.0000 18.9617 0.5950 
0.2950 -0.2398 8.0314 1.0000 -0.1019 5.6754 1.0000 0.0000 
2 5 151.3159 0.0000 0.0000 -0.4644 0.0000 1.0000 6.0000 0.5950 
9.4365 1.0000 0.0000 1.0000 -0.0303 7.0100 1.0000 0.0000 
3 5 0.0000 0.0000 0.0000 0.5563 -0.4038 1.0000 49.5611 0.6000 
0.4259 -0.4577 12.7569 1.0000 -0.1100 7.1145 1.0000 0.0000 
4 5 0.0000 0.0000 0.0000 0.4438 -0.2034 1.0000 40.3399 0.6000 
0.3296 -0.3153 9.1227 1.0000 -0.1805 5.6864 1.0000 0.0000 
5 5 96.1871 93.7006 68.6860 0.0955 -0.4781 1.0000 17.8574 0.6000 
0.2723 -0.2373 9.7875 1.0000 -0.0950 6.4757 1.0000 0.0000 
1 6 90.6281 6.3660 0.0000 0.3176 -0.5558 1.0000 17.2117 0.5577 
0.7223 -0.2118 7.7440 1.0000 -0.1039 5.4442 1.0000 0.0000 
2 6 137.1002 0.0000 0.0000 -0.1902 0.0000 1.0000 6.0000 0.4256 
17.7186 1.0000 0.0000 1.0000 -0.0377 6.4281 0.0000 0.0000 
3 6 230.7615 93.6959 43.3991 -0.3617 -0.3000 1.0000 36.0000 0.3161 
0.9856 -0.3882 4.6686 1.0000 -0.3960 4.5499 1.0000 0.0000 
6 6 72.8867 50.0318 30.0000 0.9983 -0.3000 1.0000 16.0000 0.1000 
1.0538 -0.0447 10.6176 1.0000 -0.1452 8.0404 0.0000 0.0000 
11 ! Nr of off-diagonal terms; Ediss;Ro;gamma;rsigma;rpi;rpi2 
1 2 0.1219 1.4000 9.8442 1.1203 -1.0000 -1.0000 
2 3 0.0344 1.6800 10.3247 0.9013 -1.0000 -1.0000 
2 4 0.1059 1.8290 9.7818 0.9598 -1.0000 -1.0000 
1 3 0.1131 1.8523 9.8442 1.2775 1.1342 1.0621 
1 4 0.1447 1.8766 9.7990 1.3436 1.1885 1.1363 
3 4 0.1048 2.0003 10.1220 1.3173 1.1096 1.0206

1 5 0.1997 2.0109 9.8603 1.6611 1.3423 -1.0000 
2 5 0.0938 1.8133 9.6519 1.3629 -1.0000 -1.0000 
1 6 0.0250 1.7695 12.4753 1.5866 1.4409 -1.0000 
2 6 0.0291 1.6805 12.5137 1.3429 -1.0000 -1.0000 
3 6 0.1958 1.7958 11.1207 1.6105 1.1632 -1.0000 
71 ! Nr of angles;at1;at2;at3;Thetao,o;ka;kb;pv1;pv2 
1 1 1 67.2326 22.0695 1.6286 0.0000 1.7959 15.4141 1.8089 
1 1 2 65.2527 14.3185 6.2977 0.0000 0.5645 0.0000 1.1530 
2 1 2 70.0840 25.3540 3.4508 0.0000 0.0050 0.0000 3.0000 
1 2 2 0.0000 0.0000 6.0000 0.0000 0.0000 0.0000 1.0400 
1 2 1 0.0000 3.4110 7.7350 0.0000 0.0000 0.0000 1.0400 
2 2 2 0.0000 27.9213 5.8635 0.0000 0.0000 0.0000 1.0400 
1 1 3 49.5561 7.3771 4.9568 0.0000 0.7533 15.9906 1.0010 
3 1 3 77.1171 39.8746 2.5403 -24.3902 1.7740 -42.9758 2.1240 
1 1 4 66.1305 12.4661 7.0000 0.0000 3.0000 50.0000 1.1880 
3 1 4 73.9544 12.4661 7.0000 0.0000 3.0000 0.0000 1.1880 
4 1 4 64.1581 12.4661 7.0000 0.0000 3.0000 0.0000 1.1880 
2 1 3 65.0000 14.2057 4.8649 0.0000 0.3504 0.0000 1.7185 
2 1 4 74.2929 31.0883 2.6184 0.0000 0.0755 0.0000 1.0500 
1 2 4 0.0000 0.0019 6.3000 0.0000 0.0000 0.0000 1.0400 
1 3 1 74.3994 44.7500 0.7982 0.0000 3.0000 0.0000 1.0528 
1 3 3 77.9854 36.6201 2.0201 0.0000 0.7434 67.0264 3.0000 
1 3 4 82.4890 31.4554 0.9953 0.0000 1.6310 0.0000 1.0783 
3 3 3 80.7324 30.4554 0.9953 0.0000 1.6310 50.0000 1.0783 
3 3 4 84.3637 31.4554 0.9953 0.0000 1.6310 0.0000 1.0783 
4 3 4 89.7071 31.4554 0.9953 0.0000 1.6310 0.0000 1.1519 
1 3 2 71.5018 21.7062 0.4735 0.0000 0.5186 0.0000 1.1793 
2 3 3 84.9468 23.3540 1.5057 0.0000 2.6374 0.0000 1.3023 
2 3 4 75.6201 18.7919 0.9833 0.0000 0.1218 0.0000 1.0500 
2 3 2 77.0645 10.4737 1.2895 0.0000 0.9924 0.0000 1.1043 
1 4 1 66.0330 22.0295 1.4442 0.0000 1.6777 0.0000 1.0500 
1 4 3 103.3204 33.0381 0.5787 0.0000 1.6777 0.0000 1.0500 
1 4 4 104.1335 8.6043 1.6495 0.0000 1.6777 0.0000 1.0500 
3 4 3 74.1978 42.1786 1.7845 -18.0069 1.6777 0.0000 1.0500 
3 4 4 74.8600 43.7354 1.1572 -0.9193 1.6777 0.0000 1.0500 
4 4 4 75.0538 14.8267 5.2794 0.0000 1.6777 0.0000 1.0500 
1 4 2 69.1106 25.5067 1.1003 0.0000 0.0222 0.0000 1.0369 
2 4 3 81.3686 40.0712 2.2396 0.0000 0.0222 0.0000 1.0369 
2 4 4 83.0104 43.4766 1.5328 0.0000 0.0222 0.0000 1.0500 
2 4 2 70.8687 12.0168 5.0132 0.0000 0.0222 0.0000 1.1243 
1 2 3 0.0000 25.0000 3.0000 0.0000 1.0000 0.0000 1.0400 
1 2 4 0.0000 0.0019 6.0000 0.0000 0.0000 0.0000 1.0400 
1 2 5 0.0000 0.0019 6.0000 0.0000 0.0000 0.0000 1.0400 
3 2 3 0.0000 0.0148 6.0000 0.0000 0.0000 0.0000 1.0400 
3 2 4 0.0000 0.0019 6.0000 0.0000 0.0000 0.0000 1.0400 
4 2 4 0.0000 0.0019 6.0000 0.0000 0.0000 0.0000 1.0400 
2 2 3 0.0000 9.7025 6.0000 0.0000 0.0000 0.0000 1.0400 
2 2 4 0.0000 0.0019 6.0000 0.0000 0.0000 0.0000 1.0400 
1 1 5 73.9923 24.7559 1.8287 0.1463 0.0059 0.0000 1.0600 
1 5 1 86.7521 36.5756 2.0199 0.1463 0.0058 0.0000 1.0600 
2 1 5 75.1310 24.8619 1.8104 0.0000 0.0050 0.0000 1.0600 
1 5 2 85.3326 36.9451 2.1403 0.0000 0.0388 0.0000 1.0706 
1 5 5 86.0081 37.0451 2.1403 0.1463 0.1070 0.0000 1.0098 
2 5 2 92.9959 36.9602 2.0403 0.0000 0.0050 0.0000 1.0200 
2 5 5 83.2918 36.9451 2.0199 0.0000 0.0050 0.0000 1.0600 
2 2 5 0.0000 0.0019 6.0000 0.0000 0.0000 0.0000 1.0400 
6 6 6 71.6771 13.0081 3.6376 0.0000 0.2384 0.0000 1.3185 
2 6 6 89.1207 11.7566 1.1579 0.0000 0.0100 0.0000 1.2975 
2 6 2 26.3763 5.5393 0.9656 0.0000 2.3381 0.0000 1.1704 
3 6 6 85.6335 17.1826 6.5759 0.0000 0.4105 0.0000 1.6398

2 6 3 59.6558 6.8748 7.0452 0.0000 4.0000 0.0000 1.0400 
3 6 3 72.7359 17.5203 2.4434 0.0000 0.0100 0.0000 1.7374 
6 3 6 18.3653 5.7702 3.4915 0.0000 4.0000 0.0000 1.9438 
2 3 6 57.5894 40.0000 8.0000 0.0000 3.8263 0.0000 1.0534 
3 3 6 54.5893 38.8349 7.6245 0.0000 2.7656 0.0000 3.0000 
2 2 6 0.0000 47.1300 6.0000 0.0000 1.6371 0.0000 1.0400 
6 2 6 0.0000 31.5209 6.0000 0.0000 1.6371 0.0000 1.0400 
3 2 6 0.0000 31.0427 4.5625 0.0000 1.6371 0.0000 1.0400 
1 1 6 63.8858 35.1811 0.6236 0.0000 2.6344 0.0000 2.3890 
1 6 1 71.6429 31.1160 0.5107 0.0000 0.0100 0.0000 1.9113 
6 1 6 63.2523 33.3810 2.2952 0.0000 0.0201 0.0000 1.7191 
1 6 6 70.9876 29.7098 1.0210 0.0000 0.0100 0.0000 1.8242 
2 1 6 96.9319 10.9008 1.4627 0.0000 2.4557 0.0000 1.5109 
1 6 2 73.9320 16.6559 3.0433 0.0000 0.7961 0.0000 1.4005 
1 3 6 91.5678 5.9243 2.4284 0.0000 2.9840 0.0000 1.0400 
1 6 3 96.3796 36.5757 0.8505 0.0000 3.6964 0.0000 1.6527 
3 1 6 42.5553 40.0000 1.5855 0.0000 1.0802 0.0000 1.1584 
34 ! Nr of torsions;at1;at2;at3;at4;;V1;V2;V3;V2(BO);vconj;n.u;n 
1 1 1 1 -0.2500 11.5822 0.1879 -4.7057 -2.2047 0.0000 0.0000 
1 1 1 2 -0.2500 31.2596 0.1709 -4.6391 -1.9002 0.0000 0.0000 
2 1 1 2 -0.1770 30.0252 0.4340 -5.0019 -2.0697 0.0000 0.0000 
1 1 1 3 -0.7098 22.2951 0.0060 -2.5000 -2.1688 0.0000 0.0000 
2 1 1 3 -0.3568 22.6472 0.6045 -4.0088 -1.0000 0.0000 0.0000 
3 1 1 3 -0.0528 6.8150 0.7498 -5.0913 -1.0000 0.0000 0.0000 
1 1 3 1 2.0007 25.5641 -0.0608 -2.6456 -1.1766 0.0000 0.0000 
1 1 3 2 -1.1953 42.1545 -1.0000 -8.0821 -1.0000 0.0000 0.0000 
2 1 3 1 -0.9284 34.3952 0.7285 -2.5440 -2.4641 0.0000 0.0000 
2 1 3 2 -2.5000 79.6980 1.0000 -3.5697 -2.7501 0.0000 0.0000 
1 1 3 3 -0.0179 5.0603 -0.1894 -2.5000 -2.0399 0.0000 0.0000 
2 1 3 3 -0.5583 80.0000 1.0000 -4.4000 -3.0000 0.0000 0.0000 
3 1 3 1 -2.5000 76.0427 -0.0141 -3.7586 -2.9000 0.0000 0.0000 
3 1 3 2 0.0345 78.9586 -0.6810 -4.1777 -3.0000 0.0000 0.0000 
3 1 3 3 -2.5000 66.3525 0.3986 -3.0293 -3.0000 0.0000 0.0000 
1 3 3 1 2.5000 -0.5332 1.0000 -3.5096 -2.9000 0.0000 0.0000 
1 3 3 2 -2.5000 3.3219 0.7180 -5.2021 -2.9330 0.0000 0.0000 
2 3 3 2 2.2500 -6.2288 1.0000 -2.6189 -1.0000 0.0000 0.0000 
1 3 3 3 0.0531 -17.3983 1.0000 -2.5000 -2.1584 0.0000 0.0000 
2 3 3 3 0.4723 -12.4144 -1.0000 -2.5000 -1.0000 0.0000 0.0000 
3 3 3 3 -2.5000 -25.0000 1.0000 -2.5000 -1.0000 0.0000 0.0000 
0 1 2 0 0.0000 0.0000 0.0000 0.0000 0.0000 0.0000 0.0000 
0 2 2 0 0.0000 0.0000 0.0000 0.0000 0.0000 0.0000 0.0000 
0 2 3 0 0.0000 0.1000 0.0200 -2.5415 0.0000 0.0000 0.0000 
0 1 1 0 0.0000 50.0000 0.3000 -4.0000 -2.0000 0.0000 0.0000 
0 3 3 0 0.5511 25.4150 1.1330 -5.1903 -1.0000 0.0000 0.0000 
0 1 4 0 -2.4242 128.1636 0.3739 -6.6098 -2.0000 0.0000 0.0000 
0 2 4 0 0.0000 0.1000 0.0200 -2.5415 0.0000 0.0000 0.0000 
0 3 4 0 1.4816 55.6641 0.0004 -7.0465 -2.7831 0.0000 0.0000 
0 4 4 0 -0.3244 27.7086 0.0039 -2.8272 -2.0000 0.0000 0.0000 
4 1 4 4 -5.5181 8.9706 0.0004 -6.1782 -2.0000 0.0000 0.0000 
0 1 5 0 0.1515 29.0501 0.0792 -4.5064 -1.0200 0.0000 0.0000 
0 5 5 0 -0.0054 0.1000 0.1715 -2.2256 -1.0000 0.0000 0.0000 
0 2 5 0 0.0000 0.0000 0.0000 0.0000 0.0000 0.0000 0.0000 
0 ! Nr of hydrogen bonds;at1;at2;at3;Rhb;Dehb;vhb1 
3 2 3 1.9682 -4.4628 1.7976 3.0000 
3 2 4 2.0000 -6.0000 1.7976 3.0000 
4 2 3 1.2000 -2.0000 1.7976 3.0000 
4 2 4 1.2979 -6.0000 1.7976 3.0000 
3 2 5 1.5000 -2.0000 1.7976 3.0000 
4 2 5 1.5000 -2.0000 1.7976 3.0000 
5 2 3 1.5000 -2.0000 1.7976 3.0000

5 2 4 1.5000 -2.0000 1.7976 3.0000	 
5 2 5 1.5000 -2.0000 1.7976 3.0000