Supporting Information for:

Thiophene/Selenophene-Based S-Shaped Double Helicenes:

Regioselective Synthesis and Structures

Mengjie Wang,‡ Lanping Dang,‡ Wan Xu, Zhiying Ma, Liuliu Shao, Guangxia Wang, Chunli Li * and Hua Wang*

Engineering Research Center for Nanomaterials, Henan University, Kaifeng, 475004, P. R. China

E-mail: chunli79@126.com; hwang@henu.edu.cn

‡ These authors contributed equally to this work.

Table of Contents

| 1. NMR and HRMS Spectra | S2 |
| --- | --- |
| 2. Fluorescence Spectra and Fluorescence Quantum Yield | S9 |
| 3. Theoretical Study | S10 |
| Orbital-Weighted Fukui Function | S10 |
| Calculated HOMO and LUMO energy | S11 |
| 4. X-ray Crystallographic Data | S12 |
| Complete Crystal Data for DH-1 | S12 |
| Complete Crystal Data for DH-2 | S14 |

- NMR and HRMS Spectra

NMR and HRMS Spectra of 5a

Figure S1. 1H NMR (400 MHz, CDCl3) spectrum of 5a

Figure S2. 13C NMR (100 MHz, CDCl3) spectrum of 5a

Figure S3. HRMS data of 5a

NMR and HRMS Spectra of 5b

Figure S4. 1H NMR (300 MHz, CDCl3) spectrum of 5b

Figure S5. 13C NMR (150 MHz, C2D2Cl4) spectrum of 5b

Figure S6. HRMS spectrum of 5b

NMR and HRMS Spectra of 5c

Figure S7. 1H NMR (400 MHz, CDCl3) spectrum of 5c

Figure S8. HRMS spectrum and data of 5c

NMR and HRMS Spectra of DH-1

Figure S9. 1H NMR (400 MHz, CDCl3) spectrum of DH-1

Figure S10. 13C NMR (100 MHz, CDCl3) spectrum of DH-1

Figure S11. HRMS data of DH-1

NMR and HRMS Spectra of DH-2

Figure S12. 1H NMR (400 MHz, CDCl3) spectrum of DH-2

Figure S13. 13C NMR (100 MHz, CDCl3) spectrum of DH-2

Figure S14. HRMS spectrum of DH-2

NMR and HRMS Spectra of DH-3

Figure S15. 1H NMR (300 MHz, CDCl3) spectrum of DH-3

Figure S16. 13C NMR (100 MHz, CDCl3) spectrum of DH-3

Figure S17. HRMS spectrum and data of DH-3

- Fluorescence Spectra and Fluorescence Quantum Yield

Figure S18. Fluorescence spectra of DH-(1-3) at room temperature in dichloromethane

([C] = 1 × 10-5 M, λex = 350 nm, slit: 1/1 nm).

Figure S19. Excitation spectra of compound DH-(1-3) in dichloromethane and quinine sulfate dehydrate in 0.1N H2SO4. (λex = 350 nm, [C] = 1 × 10-5 M).

Table S1.The fluorescence quantum yield (Ф) of DH-(1-3) calculated according to the formula: ΦF = (nx/ns)2As/Ax Dx/DsΦs

| Compound | Peak Area(D) | Refractive index(n) | Yeild(Φ) |
| --- | --- | --- | --- |
| DH-1 | 1.6×104 | 1.42 | 0.0123 |
| DH-2 | 2.3×103 | 1.42 | 0.0016 |
| DH-3 | 2.4×103 | 1.42 | 0.0017 |
| Quinine sulfate | 8.4×105 | 1.33 | 0.54 |

- Theoretical Study

Orbital-Weighted Fukui Function of 5a

Figure S20. Orbital-Weighted Fukui Function of 5a.

Figure S21. Orbital-Weighted Fukui Function of closing one benzene compound.

Calculated HOMO and LUMO Energy

| DH-1_HOMO | DH-1_LUMO |
| --- | --- |
| DH-2_HOMO | DH-2_LUMO |
| DH-3_HOMO | DH-3_LUMO |

Figure S22. The contour plots of the HOMOs and LUMOs for DH-1, DH-2, and DH-3.

Table S2. Calculated HOMO and LUMO energy level and energy gap at B3LYP/6-31G** level of theory and the optical band gaps estimated from the absorption edges.

| Compounds | LUMO (eV) theory | HOMO (eV) theory | Eg (eV) theory | λonset (nm) experimental | Egopt (eV) experimental |
| --- | --- | --- | --- | --- | --- |
| DH-1 | -1.42 | -5.39 | 3.97 | 403 | 3.08 |
| DH-2 | -1.49 | -5.32 | 3.83 | 412 | 3.01 |
| DH-3 | -1.47 | -5.28 | 3.81 | 416 | 2.98 |

- X-ray crystallographic data

Complete crystal data for DH-1

Table S3. Crystal data and structure refinement for DH-1.

Identification code 	DH-1

Empirical formula 	C32H26S6Si2

Formula weight 	659.07

Temperature 	150.0 K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 11.1290(7) Å	α = 108.362(2)°

b = 12.1240(7) Å	β = 111.318(2)°

c = 13.7363(9) Å	γ = 100.961(2)°

Volume	1538.32(17) Å3

Z	2

Density (calculated)	1.423 Mg/m3

Absorption coefficient	0.546 mm-1

F(000)	684

Crystal size	0.14 x 0.12 x 0.08 mm3

Theta range for data collection	2.284 to 25.499°

Index ranges	-13 ≤ h ≤ 13, -14 ≤ k ≤ 13, -16 ≤ l ≤16

Reflections collected	19274

Independent reflections	5716 [R(int) = 0.1014]

Completeness to theta = 25.242°	99.7 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.7457 and 0.6783

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	5716 / 0 / 367

Goodness-of-fit on F2	1.047

Final R indices [I>2sigma(I)]	R1 = 0.0562, wR2 = 0.0872

R indices (all data)	R1 = 0.1093, wR2 = 0.1101

Extinction coefficient	n / a

Largest diff. peak and hole	0.476 and -0.451 e.Å-3

Figure S23. The crystal structures for compound DH-1. Carbon, sulfur, and silicon atoms are depicted with thermal ellipsoids set at 30% probability level, and all hydrogen atoms are omitted for clarity.

Figure S24. Molecular configuration of DH-1 in one unit cell.

Figure S25. Multiple interactions in the crystal packings of DH-1.

Figure S26. Molecular packing of DH-1.

Complete crystal data for DH-2

Table S4. Crystal data and structure refinement for DH-2.

Identification code 	DH-2

Empirical formula 	C32H26S2Se4Si2

Formula weight 	846.67

Temperature 	149.98 K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 11.0959(11) Å	α = 112.217(4)°.

b = 12.2773(12) Å	β = 106.495(3)°.

c = 13.5535(13) Å	γ = 99.898(3)°.

Volume	1555.7(3) Å3

Z	2

Density (calculated)	1.807 Mg/m3

Absorption coefficient	4.951 mm-1

F(000)	828

Crystal size	0.21 x 0.17 x 0.12 mm3

Theta range for data collection	2.288 to 28.326°.

Index ranges	-14 ≤ h ≤ 14, -15 ≤ k ≤ 16, -18 ≤ l ≤ 18

Reflections collected	23440

Independent reflections	7708 [R(int) = 0.0726]

Completeness to theta = 25.242°	99.7 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.7457 and 0.5103

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7708 / 0 / 367

Goodness-of-fit on F2	1.027

Final R indices [I>2sigma(I)]	R1 = 0.0443, wR2 = 0.0999

R indices (all data)	R1 = 0.0690, wR2 = 0.1133

Extinction coefficient	n/a

Largest diff. peak and hole	1.175 and -0.880 e.Å-3

Figure S27. The crystal structures for compound DH-2. Carbon, selenium, sulfur, and silicon atoms are depicted with thermal ellipsoids set at 30% probability level, and all hydrogen atoms are omitted for clarity.

Figure S28. Molecular configuration of DH-2 in one unit cell.

Figure S29. Multiple interactions in the crystal packings of DH-2

Figure S30. Molecular packing of DH-2.