Supporting Information for

Organic Thermally Activated Delayed Fluorescence Material with Strained Benzoguanidine Donor

Alexander C. Brannan,  Elvie F. P. Beaumont, Nguyen Le Phuoc, George F. S. Whitehead*, Mikko Linnolahti*  and Alexander S. Romanov*

Figure S1. 1H NMR spectrum of 4BGIPN							2

Figure S2. 13C NMR spectrum of 4BGIPN							2

Figure S3. Thermogravimetric analysis for compound 4BGIPN.				3

Figure S4. An overlay of the X-ray crystal structure and optimised S0 geometry of compound 4BGIPN.											3

Photophysical Characterisation								3

Table S1. HOMO and LUMO molecular orbitals						4

Tables S2. Dipole moments in S0 and S1 states in S0 geometry				4

Table S3. Vertical excitations S0 → S1 and S0→ Tn, character and oscillator strength coefficients for S0 → S1.									4

Table S4. HONTO andd LUNTO molecular orbitals of the excited states.			4

Coordinates for compound 4BGIPN								7

Figure S1. 1H NMR (DMSO-d6) spectrum of 4BGIPN.

Figure S2. 13C NMR (DCM-d2) spectrum of 4BGIPN

Figure S1. Thermogravimetric analysis for compound 4BGIPN.

Figure S2. An overlay of the X-ray crystal structure and optimised S0 geometry of compound 4BGIPN.

Photophysical Characterisation.

UV-visible absorption spectra were recorded using a Varian Cary 5000 UV-Vis-NIR spectrometer. Photoluminescence measurements were recorded on an Edinburgh Instruments FLS980 spectrometer with a solids mount attachment where appropriate. Absolute photoluminescence quantum yields were recorded using Hamamatsu Quantaurus-QY C11347-11. Quantum yields have been measured in air for solid samples and under nitrogen for solutions. Time resolved luminescence data were collected on a time-correlated single photon counting (TCSPC) Edinburgh Instruments FLS980 spectrometer using F-900 software. A xenon flash lamp and EPL pulsed diode lasers were used as excitation sources. The collected data were analysed using F-900 software.

Computational Details.

Table S1. HOMO and LUMO molecular orbitals in crystal and optimized S0 geometry.

|  | HOMO | LUMO |
| --- | --- | --- |
| (crystal) Overlap integral: 0.27 |  |  |
| (opt) Overlap integral: 0.29 |  |  |

Tables S2. Dipole moments in S0 and S1 states in crystal and optimized S0 geometry.

|  | S0 | S1 |
| --- | --- | --- |
| (crystal) | 6.7D | 13.6D |
| (opt) | 6.4D | 7.2D |

Table S3. Vertical excitations S0 → S1 and S0→ Tn, character and oscillator strength coefficients for S0 → S1 in crystal and optimized S0 geometry.

|  | Excitation energy | Character | Oscillator strength |
| --- | --- | --- | --- |
| (crystal) | S1: 3.11eV = 399nm | HOMO – LUMO (92%) | 0.0773 |
|  | T1: 2.94eV = 422nm | HOMO – LUMO (71%) |  |
|  | T2: 3.09eV = 402nm | HOMO-2 – LUMO (19%) HOMO-1 – LUMO (19%) |  |
|  | T3: 3.13eV = 396nm | HOMO-2 – LUMO (47%) |  |
| (opt) | S1: 3.19eV = 388nm | HOMO – LUMO (78%) | 0.0906 |
|  | T1: 2.99eV = 415nm | HOMO – LUMO (46%) HOMO-1 – LUMO (18%) |  |
|  | T2: 3.05eV = 406nm | HOMO – LUMO (35%) HOMO-3 – LUMO (19%) HOMO – LUMO+1 (16%) |  |
|  | T3: 3.18eV = 389nm | HOMO-1 – LUMO (50%) HOMO – LUMO+1 (31%) |  |

Table S4. HONTO and LUNTO molecular orbitals of the excited states in crystal and optimized S0 geometry.

|  |  | HONTO | LUNTO |
| --- | --- | --- | --- |
| (crystal) | S1 |  |  |
|  | T1 |  |  |
|  | T2 |  |  |
|  | T3 |  |  |
| (opt) | S1 |  |  |
|  | T1 |  |  |
|  | T2 |  |  |
|  | T3 |  |  |

Coordinates for compound 4BGIPN in the ground state S0 geometry (crystal geometry).

N                 14.31500000    9.19000000    7.14100000

N                 10.55200000   13.38100000    7.44200000

N                  9.72700000   10.69700000    6.79700000

N                  7.74300000    9.98600000    7.53600000

N                  9.48500000    9.18400000    8.75300000

N                  8.82600000   12.44200000    8.95700000

N                 13.24800000   13.72600000    8.36300000

N                  8.97500000   14.65100000    8.38400000

N                 11.54000000   14.19500000   10.08800000

N                 15.93700000   10.16600000    5.55500000

N                 16.09200000    8.04800000    6.42700000

N                 13.14800000   15.68000000    9.45200000

C                 12.01500000   10.00100000    6.90600000

C                  9.07200000    9.90900000    7.74300000

C                 11.49300000   12.32100000    7.39700000

N                 16.02600000   11.63900000    8.94600000

C                  7.15400000    9.27800000    8.56500000

C                 11.08200000   11.03100000    7.01200000

C                 12.82500000   12.50700000    7.81300000

C                  8.74500000   11.32800000    6.02600000

N                 11.31800000    7.70900000    5.92100000

C                  9.45200000   13.37800000    8.28800000

C                 12.56200000   14.45100000    9.32700000

C                 13.35100000   10.20600000    7.26800000

C                 15.01900000   11.56300000    8.37900000

C                  8.24900000    8.78500000    9.30700000

C                 13.73100000   11.46500000    7.76200000

C                 11.60400000    8.73400000    6.34900000

C                 15.43700000    9.28700000    6.34200000

C                  7.49200000   10.84800000    6.48100000

C                 14.26900000   14.57500000    7.86000000

C                 10.76800000   14.72000000    7.04200000

C                  7.82000000   13.17900000    9.59500000

C                 14.28400000    7.90200000    7.71400000

C                  9.81600000   15.52700000    7.66900000

C                  6.83300000   12.72200000   10.44800000

H                  6.75900000   11.80200000   10.67300000

C                  8.02300000    7.99700000   10.42100000

H                  8.74900000    7.65100000   10.92700000

C                  7.89100000   14.55400000    9.26500000

C                  8.84000000   12.17900000    4.93900000

H                  9.67800000   12.51600000    4.64300000

C                 11.70800000   15.27000000    6.19400000

H                 12.34200000   14.72800000    5.73800000

C                 15.37400000    7.20800000    7.27000000

C                  5.66100000    8.20200000   10.03500000

H                  4.77700000    7.98400000   10.30800000

C                 11.39700000   15.40800000   10.79100000

C                 14.21200000   15.80400000    8.52200000

C                  6.33500000   11.19100000    5.82400000

H                  5.48900000   10.86900000    6.11500000

C                 17.04200000    9.45900000    5.01400000

C                  6.44300000   12.03000000    4.71300000

H                  5.65700000   12.26300000    4.23300000

C                 15.18900000   14.36900000    6.82800000

H                 15.25300000   13.54100000    6.36600000

C                  5.94800000   13.66700000   10.96200000

H                  5.27300000   13.38000000   11.56600000

C                  7.03500000   15.49100000    9.77600000

H                  7.11900000   16.41600000    9.57300000

C                  5.84200000    8.98400000    8.91200000

H                  5.10700000    9.30400000    8.40300000

C                  6.73000000    7.72600000   10.77700000

H                  6.56100000    7.20000000   11.55000000

C                 17.15000000    8.16300000    5.53400000

C                  6.01300000   14.99400000   10.62700000

H                  5.36300000   15.59400000   10.97400000

C                  9.78200000   16.87200000    7.50600000

H                  9.12600000   17.40500000    7.93900000

C                  7.64200000   12.52100000    4.29800000

H                  7.66800000   13.11100000    3.55400000

C                 10.46100000   15.76700000   11.74600000

H                  9.78000000   15.16100000   12.01200000

C                 15.63300000    5.86600000    7.66900000

H                 16.37400000    5.36100000    7.35600000

C                 12.39600000   16.34100000   10.41600000

C                 11.68500000   16.64200000    6.03800000

H                 12.33000000   17.05600000    5.47800000

C                 10.74100000   17.43200000    6.68300000

H                 10.75400000   18.37400000    6.55700000

C                 17.97100000    9.91300000    4.07800000

H                 17.93800000   10.79500000    3.72300000

C                 10.54300000   17.01500000   12.29700000

H                  9.91800000   17.26000000   12.96700000

C                 11.50000000   17.93100000   11.91500000

H                 11.50000000   18.79900000   12.29800000

C                 16.00200000   15.45300000    6.52400000

H                 16.62900000   15.35800000    5.81600000

C                 13.38000000    7.35200000    8.59900000

H                 12.61700000    7.83300000    8.89900000

C                 15.05200000   16.84200000    8.24400000

H                 15.03200000   17.65400000    8.73600000

C                 12.48100000   17.58700000   10.95800000

H                 13.16600000   18.19500000   10.70600000

C                 19.02100000    7.69900000    4.24000000

H                 19.71000000    7.11400000    3.94400000

C                 18.14500000    7.25200000    5.17000000

H                 18.20300000    6.38300000    5.54700000

C                 13.64700000    6.03800000    9.03500000

H                 13.07500000    5.62500000    9.66900000

C                 18.95600000    8.99100000    3.69600000

H                 19.60000000    9.24900000    3.04600000

C                 15.95000000   16.63600000    7.18100000

H                 16.53200000   17.34100000    6.91800000

C                 14.69900000    5.37300000    8.56000000

H                 14.81900000    4.48000000    8.86200000

Coordinates for compound 4BGIPN in the ground state S0 geometry (optimized geometry).

N                  3.83442600    0.90870300   -0.29780500

N                 -1.50230400   -0.52172100    0.65031500

N                 -0.54057900    2.03640200    1.38865100

N                 -2.02326100    3.70084800    1.16456000

N                 -0.36054800    3.76416300   -0.37286600

N                 -2.68040900    1.27132700   -0.57465100

N                  0.28696900   -2.33182700   -0.65743800

N                 -3.70099500   -0.56708400    0.26534200

N                 -1.85021900   -1.91604700   -1.84132600

N                  5.04490800   -1.00589500    0.69914400

N                  6.05642500    0.74200300   -0.32996600

N                 -1.16351300   -3.95898100   -1.15101700

C                  1.64414000    1.43409500    0.60414200

C                 -0.85532500    3.18418900    0.66862000

C                 -0.15923300   -0.18673000    0.43780100

N                  3.43521500   -2.11770300   -2.11996000

C                 -2.37082900    4.72234800    0.29119800

C                  0.30649200    1.07789400    0.81955000

C                  0.71112600   -1.06550000   -0.22705000

C                 -1.57814100    1.84042000    2.32279800

N                  2.58001900    3.58120700    1.69188600

C                 -2.55406200    0.15899500    0.06996500

C                 -0.92244800   -2.61304700   -1.26797800

C                  2.50160100    0.56563000   -0.07060500

C                  2.82188800   -1.48119100   -1.38120600

C                 -1.31154600    4.74904300   -0.64703000

C                  2.02334500   -0.67187100   -0.51165900

C                  2.15008200    2.64010800    1.18556800

C                  4.90542300    0.11638500    0.06799500

C                 -2.51542900    2.87437400    2.16721500

C                  0.80584600   -3.55752900   -0.17141500

C                 -2.02293100   -1.69785500    1.21251600

C                 -4.04594900    1.30792700   -0.85426900

C                  4.34873700    2.05799600   -0.93584100

C                 -3.40397500   -1.74127100    0.94481300

C                 -4.77766300    2.28639400   -1.51968800

H                 -4.28099200    3.17104000   -1.90090000

C                 -1.34667300    5.67694200   -1.68227800

H                 -0.54657300    5.71179100   -2.40976500

C                 -4.70974200    0.16327100   -0.35022500

C                 -1.74900400    0.85408600    3.27227000

H                 -1.01696600    0.06545600    3.39977800

C                 -1.40068900   -2.69523800    1.93595500

H                 -0.34290100   -2.64702800    2.16784500

C                  5.74846200    1.94854800   -0.95596100

C                 -3.47440100    6.48812100   -0.82268200

H                 -4.30699700    7.17295000   -0.91827500

C                 -2.84145800   -2.86517100   -2.08329300

C                 -0.11428400   -4.57284400   -0.47623800

C                 -3.66516200    2.91903100    2.93185000

H                 -4.39282100    3.70876500    2.80375000

C                  6.43197700   -1.16250600    0.72938900

C                 -3.85405200    1.90316500    3.86694300

H                 -4.74852100    1.90559800    4.47556700

C                  1.95256600   -3.81980800    0.55299200

H                  2.67051400   -3.04482900    0.79758900

C                 -6.14178500    2.08549400   -1.67675300

H                 -6.73092100    2.83081900   -2.19587400

C                 -6.07028900   -0.04579400   -0.50869200

H                 -6.56019900   -0.93267600   -0.12739000

C                 -3.45718800    5.57950900    0.22685500

H                 -4.26026700    5.53953400    0.95123300

C                 -2.43441000    6.53496500   -1.75811600

H                 -2.48306900    7.25915300   -2.56143500

C                  7.09092800   -0.08123700    0.09661200

C                 -6.77779200    0.93882000   -1.18598800

H                 -7.84292200    0.81759900   -1.33548100

C                 -4.17442200   -2.81904800    1.33460000

H                 -5.22947300   -2.86684900    1.09996900

C                 -2.91152700    0.89301700    4.03943300

H                 -3.08093500    0.12361300    4.78091700

C                 -4.11925600   -2.68100800   -2.60269000

H                 -4.44071300   -1.69712200   -2.92147900

C                  6.53472100    2.92316200   -1.53872500

H                  7.61283300    2.83884500   -1.55598600

C                 -2.44164700   -4.15365800   -1.65636700

C                 -2.17937600   -3.78294600    2.33178700

H                 -1.71384700   -4.59044600    2.88183600

C                 -3.53571800   -3.84841000    2.02545300

H                 -4.11048100   -4.71085200    2.33595600

C                  7.19040400   -2.19087900    1.27865100

H                  6.70389500   -3.02672900    1.76386700

C                 -4.95699500   -3.78448400   -2.67744200

H                 -5.95695300   -3.66472400   -3.07483800

C                 -4.54038000   -5.05383700   -2.25640400

H                 -5.22366100   -5.88954300   -2.33481300

C                  2.16204900   -5.13799500    0.95563800

H                  3.05622300   -5.37780900    1.51509700

C                  3.69794300    3.13349400   -1.50719300

H                  2.61715600    3.22133900   -1.49168400

C                  0.09538300   -5.87842000   -0.07758800

H                 -0.61696000   -6.65751600   -0.31310600

C                 -3.26855500   -5.26245400   -1.74058700

H                 -2.94901700   -6.24152600   -1.40817600

C                  9.20359900   -1.03078100    0.55713800

H                 10.28418500   -1.00477400    0.50420000

C                  8.47016500    0.00708900   -0.00022300

H                  8.95627400    0.84241300   -0.48709400

C                  4.49353900    4.11538500   -2.09254100

H                  4.01753300    4.97679600   -2.54113600

C                  8.57162100   -2.11033500    1.18471300

H                  9.17877200   -2.90136800    1.60619100

C                  1.25534200   -6.14726000    0.64499200

H                  1.45441100   -7.16028200    0.96864400

C                  5.88207800    4.01458000   -2.10595700

H                  6.46771600    4.79837700   -2.56766800