Supplementary Materials for

Curcumin-loaded albumin submicron particles with their potential as a cancer therapy: an in vitro study

List of Figures

Table S1 Size and zeta potential of HSA-MPs and CUR-HSA-MPs

Figure S1 Cellular uptake of CUR at 4 h in MCF-7 cell (A), free CUR (B), HSA-MPs (C), CUR-HSA-MPs

Table S1 Size and zeta potential of HSA-MPs and CUR-HSA-MPs

| Particle | Size |  | Zeta potential |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Z-Average Size (nm) | PdI | ZP (mV) | Mob (μmCm/Vs) | Cond (mS/cm) |
| HSA-MPs | 888.88 ± 64 | 0.3 ± 0.14 | -14.50 ± 0.6 | -1.12 ± 0.05 | 18.38 ± 0.18 |
| CUR-HSA-MPs | 983.57 ± 82 | 0.31 ± 0.13 | -15.34 ± 0.2 | -1.21 ± 0.01 | 18.10 ± 0.07 |

Data are presented as mean ± SD. (n = 3); Conductivity (Cond), electrophoretic mobility unit (Mob), polydispersity index (PdI), and zeta potential (ZP).

Figure S1 Cellular uptake of CUR at 4 h in MCF-7 cell (A), free CUR (B), HSA-MPs (C), CUR-HSA-MPs in MCF-7 cell using fluorescence microscopy. A and B shows fluorescent images of non-treated and free curcumin-treated samples to verify the presence of cell autofluorescence. C imaged the internalization of HSA-MPs-FITC, which can be seen the fluorescence is diffused throughout the cytoplasm.

|  | Bright fild | FITC | Merge |
| --- | --- | --- | --- |
| A |  |  |  |
| B |  |  |  |
| C |  |  |  |
| D |  |  |  |