Z-Selective Semihydrogenation of Alkynes via Ni/Lewis Acid Synergistic Catalyzed System Using DMF as Hydrogen Source and Solvent

Lei Kang*a,b, Haifeng Gaob, Luo Yang*b

aSchool of Surveying & Testing, Shaanxi Railway Institute, Weinan, 714000, China.

bKey Laboratory for Green Organic Synthesis and Application of Hunan Province, College of Chemistry, Xiangtan University, Hunan, 411105, China.

Corresponding Authors

*Lei Kang. E-mail: kanglei@gzhu.edu.cn

*Luo Yang. E-mail: yangluo@xtu.edu.cn

1.General information

Thin-layer chromatography (TLC) was performed using E. Merck Silica Gel 60 F254 precoated plates (0.25 mm). The developed chromatography was analyzed by UV lamp (254 nm). Nuclear magnetic resonance (NMR) spectra were recorded on a Bruker Avance 400 spectrometer at ambient temperature. Chemical shifts for 1H NMR spectra are reported in parts per million (ppm) from tetramethylsilane with the solvent resonance as the internal standard (chloroform: δ 7.26 ppm). Chemical shifts for 13C NMR spectra are reported in parts per million (ppm) from tetramethylsilane with the solvent as the internal standard (CDCl3: δ 77.16 ppm). Data are reported as following: chemical shift, multiplicity (s = singlet, d = doublet, dd = doublet of doublets, t = triplet, q = quartet, m = multiplet, br = broad signal), coupling constant (Hz), and integration. The Z/E stereoisomeric ratio of the product was determined by gas chromatography (GC) analysis of the crude reaction mixture.

2.Experimental Section

An oven-dried reaction vessel was charged with diphenylacetylene (0.2 mmol, 35.6 mg), Zn(OAc)2·2H2O (50 mol%, 22 mg), and NiCl2 (20 mol%, 3.3 mg). DMF (0.8 mL) was then added, the vessel was sealed, and the mixture was stirred and heated at 150 °C (oil bath temperature) for 24 h. The reaction was monitored by GC analysis; upon complete consumption of the starting material, heating was discontinued. After cooling to room temperature, the volatiles were removed under reduced pressure. The resulting crude residue was purified by flash column chromatography on silica gel (eluent: petroleum ether) to afford pure (Z)-stilbene (2a) as a colorless solid in 95% isolated yield (34.4 mg). The Z/E ratio (98:2) was determined by GC analysis of the crude mixture.

3.Spectra data of products 2a-2p

(2a)1

Yellow oil. 1H NMR (400 MHz, CDCl3, TMS) δ 7.24-7.17 (m, 10H), 6.60 (s, 2H);

13C NMR (100 MHz, CDCl3) δ 137.35, 130.37, 128.99, 128.33, 127.21.

(2b)2

1H NMR (400 MHz, CDCl3, TMS) δ 7.30 – 7.17 (m, 5H), 7.17 – 7.10 (m, 2H), 7.02 (d, J = 7.9 Hz, 2H), 6.55 (s, 2H), 2.31 (s, 3H).

13C NMR (100 MHz, CDCl3) δ 137.53, 136.90, 134.29, 130.23, 129.58, 128.94, 128.88, 128.82, 128.22, 127.00, 21.27.

(2c)1

1H NMR (400 MHz, CDCl3, TMS) δ 7.16 (d, 2H, J = 8.1 Hz), 7.03 (d, 2H, J = 7.9 Hz), 6.60 (s, 2H);

13C NMR (100 MHz, CDCl3) δ 136.75, 134.51, 129.53, 128.90, 128.77, 21.26.

(2d)1

1H NMR (400 MHz, CDCl3, TMS) δ 7.50 – 6.91 (m, 7H), 6.75 (d, J = 8.8 Hz, 2H), 6.52 (d, J = 1.8 Hz, 2H), 3.78 (s, 3H).

13C NMR (100 MHz, CDCl3) δ 158.69, 137.64, 130.17, 129.79, 129.68, 128.84, 128.78, 128.25, 126.92, 113.61, 55.21.

(2e)2

1H NMR (400 MHz, CDCl3) δ 7.34 – 7.17 (m, 5H), 7.09 (m, 4H), 6.60 (s, 2H), 2.29 (s, 3H).

13C NMR (100 MHz, CDCl3) δ 137.84, 137.41, 137.27, 130.45, 130.16, 129.69, 128.97, 128.24, 128.17, 127.94, 127.14, 125.96, 21.43.

(2f)2, 3

1H NMR (400 MHz, CDCl3) δ 7.47 (d, J = 8.2 Hz, 2H), 7.34 (d, J = 8.4 Hz, 2H), 7.30 – 7.17 (m, 5H), 6.73 (d, J = 12.3 Hz, 1H), 6.60 (d, J = 12.3 Hz, 1H).

13C NMR (100 MHz, CDCl3) δ 140.92, 136.56, 132.34, 129.14, 128.82, 128.75, 128.43, 127.58, 125.16 (q, J1 = 3.7, J2 = 3.8 Hz), 122.83.

(2g)4

1H NMR (400 MHz, CDCl3) δ δ 7.34 (d, J = 8.4 Hz, 2H), 7.25 – 7.20 (m, 5H), 7.10 (d, J = 8.3 Hz, 2H), 6.63 (d, J = 12.2 Hz, 1H), 6.50 (d, J = 12.2 Hz, 1H).

13C NMR (100 MHz, CDCl3) δ 136.86, 136.14, 131.39, 131.07, 130.57, 128.97, 128.83, 128.38, 127.38, 120.96.

(2h)2

1H NMR (400 MHz, CDCl3) δ 7.35 – 7.03 (m, 9H), 6.68 (d, J = 12.2 Hz, 1H), 6.55 (d, J = 12.2 Hz, 1H).

13C NMR (100 MHz, CDCl3) δ 139.17, 136.68, 134.13, 131.64, 129.50, 128.91, 128.89, 128.78, 128.40, 127.52, 127.20, 127.07.

(2i)5

1H NMR (400 MHz, CDCl3) δ 7.23 (d, J = 8.5 Hz, 4H), 7.17 (d, J = 8.4 Hz, 4H), 6.58 (s, 2H).

13C NMR (100 MHz, CDCl3) δ 135.29, 133.06, 130.17, 129.64, 128.58.

(2j)2

1H NMR (400 MHz, CDCl3) δ 7.35 – 7.08 (m, 9H), 6.62 (d, J = 12.2 Hz, 1H), 6.53 (d, J = 12.2 Hz, 1H).

13C NMR (100 MHz, CDCl3) δ 136.90, 135.68, 132.77, 130.98, 130.25, 128.95, 128.84, 128.44, 128.37, 127.35.

(2k)4

1H NMR (400 MHz, CDCl3) δ 7.27 – 7.12 (m, 6H), 7.01 (d, J = 7.7 Hz, 1H), 6.97 – 6.83 (m, 2H), 6.65 (d, J = 12.2 Hz, 1H), 6.54 (d, J = 12.2 Hz, 1H).

13C NMR (100 MHz, CDCl3) δ 162.73 (d, J = 245.2 Hz), 139.51 (d, J = 7.8 Hz), 129.69 (d, J = 8.4 Hz), 129.00 (d, J = 2.2 Hz), 115.56 (d, J = 21.7 Hz), 114.01 (d, J = 21.2 Hz).

(2l)6

1H NMR (400 MHz, CDCl3) δ 7.29 – 7.07 (m, 4H), 7.00 – 6.83 (m, 4H), 6.54 (s, 2H).

13C NMR (100 MHz, CDCl3) δ 161.87 (d, J = 246.9 Hz), 132.98 (d, J = 3.4 Hz), 130.50 (d, J = 7.9 Hz), 129.11 (d, J = 1.2 Hz), 115.28 (d, J = 21.4 Hz).

(2m)4

1H NMR (400 MHz, CDCl3) δ 7.27 – 7.16 (m, 7H), 6.95 – 6.85 (m, 2H), 6.59 (d, J = 12.2 Hz, 1H), 6.53 (d, J = 12.2 Hz, 1H).

13C NMR (100 MHz, CDCl3) δ 161.85 (d, J = 246.7 Hz), 133.21 (d, J = 3.4 Hz), 130.56 (d, J = 7.8 Hz), 130.28 (d, J = 1.0 Hz), 115.18 (d, J = 21.4 Hz).

(2n)7

1H NMR (400 MHz, CDCl3) δ 7.43 – 6.97 (m, 9H), 6.64 (d, J = 12.2 Hz, 1H), 6.51 (d, J = 12.2 Hz, 1H).

13C NMR (100 MHz, CDCl3) δ 139.45, 136.61, 131.79, 131.66, 130.08, 129.74, 128.86, 128.64, 128.36, 127.51, 127.47, 122.31.

(2o)7

1H NMR (400 MHz, CDCl3) δ 7.36 (d, J = 8.5 Hz, 4H), 7.08 (d, J = 8.5 Hz, 4H), 6.54 (s, 2H).

13C NMR (100 MHz, CDCl3) δ 135.70, 131.68, 131.54, 130.47, 129.73, 121.25.

(2p)

1H NMR (400 MHz, CDCl3) δ 7.66 (d, J = 8.3 Hz, 2H), 7.30 (d, J = 8.1 Hz, 2H), 7.28 – 7.12 (m, 5H), 6.70 (d, J = 12.2 Hz, 1H), 6.59 (d, J = 12.2 Hz, 1H), 5.93 (d, J = 94.6 Hz, 2H).

13C NMR (100 MHz, CDCl3) δ 169.47, 141.20, 136.70, 132.10, 131.76, 129.10, 128.88, 128.39, 127.53, 127.38.

(4a)5

1H NMR (400 MHz, CDCl3) δ 7.41 – 7.22 (m, 4H), 6.75 – 6.66 (m, 1H), 5.74 (d, J = 17.6 Hz, 1H), 5.23 (d, J = 11.0 Hz, 1H).

13C NMR (100 MHz, CDCl3) δ 137.70, 137.02, 128.66, 127.94, 126.35, 113.94.

(4b)8

1H NMR (400 MHz, CDCl3) δ 7.30 (d, J = 6.3 Hz, 2H), 7.12 (d, J = 6.6 Hz, 2H), 6.80 – 6.58 (m, 1H), 5.69 (d, J = 17.7 Hz, 1H), 5.18 (d, J = 10.9 Hz, 1H), 2.33 (s, 3H).

13C NMR (100 MHz, CDCl3) δ 137.74, 136.84, 134.95, 129.35, 126.25, 112.89, 21.34.

(4c)5, 9

1H NMR (400 MHz, CDCl3) δ 7.34 (d, J = 8.9 Hz, 2H), 6.85 (d, J = 8.9 Hz, 2H), 6.65 (dd, J = 17.7, 10.9 Hz, 1H), 5.60 (d, J = 17.7 Hz, 1H), 5.12 (d, J = 11.9 Hz, 1H), 3.79 (s, 3H).

13C NMR (100 MHz, CDCl3) δ 159.49, 136.34, 130.54, 127.50, 114.02, 111.68, 55.38.

(4d)9

1H NMR (400 MHz, CDCl3) δ 7.36 (dd, J = 8.9, 5.3 Hz, 2H), 7.05 – 6.94 (m, 2H), 6.67 (dd, J = 17.6, 10.9 Hz, 1H), 5.65 (d, J = 17.6 Hz, 1H), 5.21 (d, J = 10.9 Hz, 1H).

13C NMR (100 MHz, CDCl3) δ 162.58 (d, J = 246.6 Hz), 135.79, 133.84 (d, J = 3.4 Hz), 127.84 (d, J = 8.2 Hz), 115.51 (d, J = 21.7 Hz), 113.62 (d, J = 2.4 Hz).

(4e)5, 9

1H NMR (400 MHz, CDCl3) δ 7.30 (q, J = 8.7 Hz, 4H), 6.65 (dd, J = 17.6, 10.9 Hz, 1H), 5.71 (dd, J = 17.6, 0.8 Hz, 1H), 5.25 (dd, J = 10.9, 0.7 Hz, 1H).

13C NMR (100 MHz, CDCl3) δ 136.14, 135.78, 133.54, 128.79, 127.55, 114.57.

(4f)5, 9

1H NMR (400 MHz, CDCl3) δ 7.43 (d, J = 8.4 Hz, 2H), 7.25 (d, J = 11.0 Hz, 2H), 6.63 (dd, J = 17.6, 10.9 Hz, 1H), 5.72 (d, J = 17.6 Hz, 1H), 5.26 (d, J = 10.9 Hz, 1H).

13C NMR (100 MHz, CDCl3) δ 136.57, 135.84, 131.74, 127.88, 121.72, 114.73.

References

(1) Li, J.; Hua, R.; Liu, T. Highly Chemo- and Stereoselective Palladium-Catalyzed Transfer Semihydrogenation of Internal Alkynes Affording cis-Alkenes. The Journal of Organic Chemistry 2010, 75 (9), 2966-2970. DOI: 10.1021/jo100247a.

(2) Fu, S.; Chen, N.-Y.; Liu, X.; Shao, Z.; Luo, S.-P.; Liu, Q. Ligand-Controlled Cobalt-Catalyzed Transfer Hydrogenation of Alkynes: Stereodivergent Synthesis of Z- and E-Alkenes. Journal of the American Chemical Society 2016, 138 (27), 8588-8594. DOI: 10.1021/jacs.6b04271.

(3) Wen, X.; Shi, X.; Qiao, X.; Wu, Z.; Bai, G. Ligand-free nickel-catalyzed semihydrogenation of alkynes with sodium borohydride: a highly efficient and selective process for cis-alkenes under ambient conditions. Chemical Communications 2017, 53 (39), 5372-5375, 10.1039/C7CC02140B. DOI: 10.1039/C7CC02140B.

(4) Das, M.; O’Shea, D. F. Z-Stereoselective Aza-Peterson Olefinations with Bis(trimethylsilane) Reagents and Sulfinyl Imines. Organic Letters 2016, 18 (2), 336-339. DOI: 10.1021/acs.orglett.5b03519.

(5) Xia, S.; Peng, J.; Xie, S.; Xu, T.; Li, L.; Liu, X.; Cao, D.; He, L.-N.; Li, C.-J. Copper-Catalyzed Chemoselective Hydrogenation of Unsaturated Bonds with Formic Acid/Formate as Hydrogen Donor. Organic Letters 2025, 27 (21), 5423-5428. DOI: 10.1021/acs.orglett.5c01372.

(6) Sheikh Mohammad, T.; Sakharov, P.; Raje, S.; de Ruiter, G. Z-Selective Semihydrogenation of Alkynes Catalyzed by a Co(I)PCNHCP Pincer Complex: A Simple, Fast, and Practical Methodology. ACS Catalysis 2025, 15 (7), 5370-5377. DOI: 10.1021/acscatal.5c00792.

(7) Chen, X.-B.; Zhang, J.; Sun, D.-Q.; Chen, K.-Q.; Chen, X.-Y. Phenanthrolines as Energy Transfer Photocatalysts for the E → Z Isomerization of Alkenes. Synthesis 2025, 57 (12), 1928-1935. DOI: 10.1055/a-2502-8374.

(8) Wang, Y.-H.; Liu, S.-T. Semi-reduction of alkynes catalyzed by a tri-palladium complex. Polyhedron 2025, 265, 117276. DOI: https://doi.org/10.1016/j.poly.2024.117276.

(9) Yan, Y.; Wang, P.; Han, J.; Wang, A.; Zhang, G.; Tian, Y.; Ge, Y.; Gao, W.; Wang, L.; Liu, Z.; et al. Modulating the electrocatalytic semihydrogenation selectivity of alkynes from water electrolysis using Pd-based sulfide and phosphide cathodes. Chemical Communications 2025, 61 (30), 5661-5664, 10.1039/D4CC06623E. DOI: 10.1039/D4CC06623E.